## Slide 1
High Strain Rate Forming of Sub-Scale Parts
via Vaporizing Foil Actuator (VFA)
Michael Dunkley
Advisor: Prof. Kinsey
Graduate Seminar Presentation
April 20, 2018

## Slide 2: Background
*One quadrillion BTUs, or ‘Quad’, is 8,000,000,000 gallons of gasoline
Large opportunity to recover waste heat from US industry
https://www.energy.gov/sites/prod/files/2006/Waste%20Heat%20Recovery%20TA%20Feb-13-2006.pdf

## Slide 3: Background
High Temperature Recuperator
High Temperature Microchannel Recuperator
Proposed Advantages:
Smaller
Lighter
Lower Cost
  Less Raw Materials
B. Paul, et al., Oregon State University, 2017

## Slide 4: Background
Lamina Insert
High Temperature Microchannel Recuperator:
25x10x13cm
*Designed by OSU
B. Paul, et al., Oregon State University, 2017

## Slide 5: Background
Lamina Insert:
0.5mm thick
50mm wide
178mm long
+/-5% tolerance on height feature, i.e., +/- 0.025mm
Traditional fabrication methods:
Photochemical Machining
Diffusion Brazing
Drawbacks:
Expensive
Over 50% of material is wasted
Unsure if traditional forming can achieve required tolerance and be a low cost solution

## Slide 6: Presentation Outline
Background
Motivation/Goals
Numerical Investigation
Experimental Studies
Future Work

## Slide 7: Motivation
High Strain Rate Forming:
Fast, Inexpensive, Repeatable
High strain rate forming increase forming limits of material
Two possible methods, electromagnetic forming (EMF, currently in MMM lab) and Vaporizing Foil Actuator (VFA)
Disadvantages of EMF:
Actuators tend to fail after repeated use
when magnetic pressures are increased
Only efficient with workpieces that are
electrically conductive
Limited velocity achievable
  EMF can reach 300-400m/s
  Where VFA can reach 800-900m/s
Applications:
Material forming, cutting and welding of dissimilar metals

## Slide 8: Vaporizer Foil Actuator Process Overview
From Ohio State University
A. Vivek, et al., Journal of Materials Processing Technology, 2013

## Slide 9: Goals
Use Finite Element Analysis to direct design of lamina, e.g., bending radii, forming depth and gap between punch and die
Implement VFA forming in MMM lab

## Slide 10: Numerical Approach
Lamina design provided by OSU
Rib
Emboss
Symmetry around center line to simplify model
Initial Bend Radii: 0.125mm; Modified Bend Radii: 0.25mm
Initial Forming Depth: 0.5mm; Modified Forming Depth: 0.2mm
Initial Gap: 1.1 x thickness; Modified Gap: 1 x thickness
Plane strain
Axisymmetric

## Slide 11: Failure Modes
Necking/Rupture
  Material failure due to excessive strains in forming
Springback
  Could lead to unacceptable variance in tolerance
Wrinkling
  Waviness experienced in full 3D part but not captured in our 2D model

## Slide 12: Material Properties
Inconel 625 * withstand corrosion and creep at high temperatures
Yield Strength: 586 MPa (85 ksi) at room temperature
Density: 8.44e-6 Kg/cu-mm (0.305 lb/cu-in )
Modulus of Elasticity: 207.5 GPa (30100 ksi )
Poisson’s Ratio: 0.278
Will receive Inconel 625 for material characterization
Special Metals, ‘INCONEL Alloy 625’, specialmetals.com

## Slide 13: Rib Forming
Foil:
Thickness: 0.5mm
Fixed BC on left and right sides of foil
Type of elements: CPE4R
700 elements
Dynamic, Explicate
Fixture:
Rigid body
Fixed BC
= 0.3
Punch
Rigid body
Displaced vertically
= 0.3
Gap
Deformed Foil
Initial Foil
Form Depth
Modified values:
Bend Radii: 0.25mm
Forming Depth: 0.2mm
Gap: 0.5mm (width of sheet)

## Slide 14: Rib Forming
Von Mises Stress for New and Original Radii, 0.2mm Form Depth and +0% Gap Width
0.125mm Radii
0.25mm Radii
Condition | Max Stress (MPa) | 
Form Depth, Form Gap | 0.125mm Radii | 0.25mm Radii
0.2mm Depth, 0% Gap | 748.8 | 733.8
0.2mm Depth, 10% Gap | 751.1 | 738.6
0.5mm Depth, 0% Gap | 829.0. | 796.1
0.5mm Depth, 10% Gap | 836.4 | 798.9

## Slide 15: Rib Forming
In-Plane Principal Strain for New and Original Radii
0.2mm Form Depth and +0% Gap Width
0.125mm Radii
0.25mm Radii
Condition | Max Strain | 
Form Depth, Form Gap | 0.125mm Radii | 0.25mm Radii
0.2mm Depth, 0% Gap | 0.149 | 0.140
0.2mm Depth, 10% Gap | 0.147 | 0.137
0.5mm Depth, 0% Gap | 0.367 | 0.341
0.5mm Depth, 10% Gap | 0.357 | 0.335
Large strain for 0.5mm depth

## Slide 16: Rib Forming
Springback measured from top left corner of sheet after the interaction between the punch and the sheet is removed
Condition | Springback (mm) | 
Form Depth, Form Gap | 0.125mm Radii | 0.25mm Radii
0.2mm, 0% | 0.0037 | 0.0194
0.2mm, 10% | 0.0038 | 0.0215
0.5mm, 0% | 0.0065 | 0.0133
0.5mm, 10% | 0.0072 | 0.0143
Sharper radii could benefit springback

## Slide 17: Emboss Forming
Step 1: Deformed sheet to desired depth
Step 2: Remove punch and die to observe springback
Initial Step
Die position based on form depth

## Slide 18: Emboss Forming
0.2mm Depth, 0.25mm Bend Radii, 0% Gap Width, Varied Hole Radius

## Slide 19: Emboss Forming
Stress and Strain for 6mm Radii Hole 0.25mm Bend Radii, Varied Form Depth and Gap Width
Condition | Max Stress (MPa) | 
Form Depth, Form Gap | Step 1 | Step 2
0.2mm Depth, 0% Gap | 723.4 | 569.2
0.2mm Depth, 10% Gap | 722.1 | 464.4
0.5mm Depth, 0% Gap | 789.0 | 567.2
0.5mm Depth, 10% Gap | 784.1 | 632.1
Condition | Max Strain | 
Form Depth, Form Gap | Step 1 | Step 2
0.2mm Depth, 0% Gap | 0.122 | 0.122
0.2mm Depth, 10% Gap | 0.120 | 0.120
0.5mm Depth, 0% Gap | 0.335 | 0.336
0.5mm Depth, 10% Gap | 0.317 | 0.318
Large strain for 0.5mm depth

## Slide 20: Emboss Forming
707.8
713.8
723.4
Max Stress (MPa)
2mm
4mm
6mm
Von Mises Stress with Varied Hole Diameter: 0.25mm Radii, 0.2mm Form Depth, 0% Gap

## Slide 21: Emboss Forming
0.086
0.122
2mm
4mm
6mm
Max Strain
0.098
Emboss Forming with Varied Hole Diameters 0.25mm Radii, 0.2mm Form Depth, 0% Gap

## Slide 22: Emboss Forming
Change in Height (mm)
Measured in positive
Y-direction
Measure springback after
removal of punch and die
Springback Height Change 0.25mm Radii, 0.2mm Depth, 0% Gap

## Slide 23: Emboss Forming
Springback Height Change 0.25mm Radii, 0.2mm Depth, 0% Gap
 | Springback (mm) |  | 
 | 2mm Radii | 4mm Radii | 6mm Radii
Vertical Direction (Y) | 0.0853 | 0.146 | 0.1622
Larger hole could benefit springback

## Slide 24: Emboss Forming
 | Change in Height (mm) |  | 
 | 2mm Radii | 4mm Radii | 6mm Radii
Vertical Direction (Y) | 0.0942 | 0.0298 | 0.0172
Height change across surface
Larger hole could benefit springback
Tolerance on Flat Emboss Surface

## Slide 25: VFA Experimental Set-Up
12 kW Magneform Machine
  400 kA
  7 kV
Vaporizing Foil: 5754-Aluminum: 127x25.4x0.07mm dog-bone strips
Copper bars: Highly conductive 101 Copper
Workpiece: 1100-Aluminum: 76x127x0.5mm sheets
Copper Bars
Vaporizing Foil
Workpiece
G10 Insulation
PDV hole in A2 steel plate

## Slide 26: VFA Experimental Results
Draw in of Material
Height limited by distance in set up
Coining of PDV hole into sheet
54mm
25mm

## Slide 27: VFA Experimental Results
Deformation of mesh and solid sheet of 1100-Al, 0.5mm thick at 7%
Compare deformation of solid sheet vs mesh
24mm
20mm

## Slide 28: Future Work
Perform uni-axial, plane strain and equi-biaxial tension, as well as high rate Kolsky bar test, on Inconel 625
Run Abaqus simulation with whole lamina geometry to assess all failure modes including wrinkling
Conduct experimental trials to assess consistency and repeatability
Compare theoretical and experimental results for both

## Slide 29: Questions

## Slide 30: References
A. Vivek, G.A. Taber, J.R. Johnson, S.T. Woodward, Glenn S. Daehn, “Electrically driven plasma via vaporization of metallic conductors: A tool for impulse metal working”, Journal of Materials Processing Technology 213(2013) 1311-1326
A. Vivek, S.R. Hanser, Glenn S. Daehn, “High strain rate metalworking with vaporizing foil actuator: Control of flyer velocities by varying input energy and foil thickness”, Review of Scientific Instruments 85, 075101 (2014)
B. Paul. “Low-Cost Waste Heat Recovery Using ‘Half-Array’ Microchannel Heat Exchangers”. Oregon State University, lecture
Special Metals, ‘INCONEL Alloy 625’, specialmetals.com

## Slide 31: Appendix
Cost Comparison

## Slide 32: Emboss Forming
Center of emboss hole
r
Springback leading to angled emboss feature and varied hole diameter
Punch
Die
Nodal Displacement
Magnified view of how the formed emboss will experience springback with the removal of the top die and punch