## Slide 1
A Study of Inconel 625 in both Tension and Compression at High Strain Rates using a Pulse-Heated Kolsky Bar
NIST SURF Program Final Presentation
Mentor: Dr. Steven Mates
Author: Charlie Nitschelm
Compression Specimen
Tension Specimen
Notes: Good afternoon! My name is Charlie Nitschelm and my talk will be on Inconel 625 in tension and compression under the mentorship of Dr. Steven Mates.

## Slide 2
Why Inconel 625?
Why is it useful?
High strength-to-weight ratio
The capabilities of the material as sheet metal
Oxidation and corrosion resistant
Great in high pressure and temperature environments
More resistant to creep than its competitors
What it is: Inconel is known as a nickel-based superalloy. Small amounts of niobium combine with nickel form intermetallic compounds. These compounds form small cubic crystals that inhibit slip and creep effectively at elevated temperatures
Notes: As you heard from the last talk, Inconel 625 is a super-alloy made of many different elements, but primarily nickel. Its usefulness in various industries, like aerospace and automotive, make it an extremely important material to understand. It is known to have a very high strength to weight ratio, it is oxidation and corrosion resistant and great in high pressure and temperature environments. This material is great in certain parts of rocket engines where it needs to not only survive its environment for one flight, but be able to be reused again and again like we see a lot of aerospace companies doing.

## Slide 3: Heat Exchanger Background
High Temperature Microchannel Recuperator:
25x10x13 cm
*Designed by OSU
Lamina Insert
B. Paul, et al., Oregon State University, 2017
Notes: For our purposes, we are working to better design a process to manufacture a Lamina insert for a heat exchanger. There are huge amounts of waste heat everyday around the world, whether it be coal or oil, heat exchangers would enable our waste heat to be converted back into electricity . Waste heat generators operate at high temperatures and may encounter corrosive liquids, so Inconel 625 is a perfect choice of material for this challenging environment

## Slide 4
Lamina Insert:
0.5 mm thick
50 mm wide
178 mm long
+/- 5 % tolerance on height feature, i.e., +/- 0.025 mm
Traditional fabrication methods:
Photochemical Machining
Diffusion Brazing
Drawbacks:
Expensive
Over 50 % of material is wasted
Heat Exchanger Background
Notes: This lamina insert is very thin, around .5mm thick. Its traditional methods to manufacture now are time consuming, expensive and a lot of material is wasted. Our goal in this research is to design a new manufacturing process that will cut down on costs, limit material waste, and be able to achieve the same tolerances we get with the other methods.

## Slide 5: Dynamic Forming Process
Max strain rate and T
Notes: In this Dynamic forming process, the material will be deformed very quickly, causing very high strain rates and large temperature increases due to adiabatic heating. That is the reason we will need to test this material at its limits of strain rate and heating times to understand how this material will behave under this process.

## Slide 6
Ni-Cr21-Mo9-Nb4 + minor constituents
Single phase Face Center Cubic (FCC)
Plasticity governed by forest dislocations (short range barriers) are usually strain rate and temperature sensitive
Physical Metallurgy of Inconel 625 (IN625)
Floreen, S., Fuchs, G.E and Yang, W.J., Superalloys 718, 625,
706 and Various Derivatives (TMS: Warrendale, PA, 1994).
Inconel 625 Wrought Microstructure
Notes: Inconel 625 is a single phase, face center cubic metal, and you can see a typical microstructure to the right. This clearly shows that there is no texture to the material yet, meaning it has no specific orientation it favors. We say that the grains in this material are equiaxed (e qwe axed). But, once a material is rolled into sheet metal, the material we will be testing on and what the Lamina insert will be manufactured from, it begins to show a lot of texture, stretching grains into oblong (ahb long) grains and changing their orientations to favor a specific direction. This can result in a material that shows different strength depending on which direction you test it.
Forest dislocations are networks of dislocations, more dislocations the stronger it becomes, work hardening!
Increase strain, handle more stress which is due to these dislocations
Electron back scatter diffraction (EBSD) taken in SEM, colors show the orientation of the grains within the metal.
Rolling introduced texture to the metal, which creates grains with preferred orientations which is why we need to test
Various directions to rolling. The picture was not the actual sheet metal we tested, but the metallurgy of a random metal.

## Slide 7
Testing Conditions
Equipment | Strain Rate [1/s]
MTS | 
MTS | 
Kolsky Bar | 
Equipment | Strain Rate [1/s]
MTS | 
MTS | 
Kolsky Bar | 
The Servo-Hydraulic Test Machine (MTS) can achieve low strain rates.
The Kolsky Bar can achieve high strain rates
The texture of the .5mm IN 625 sheet metal needs to be tested at different orientation to understand the effects of the new metallurgy
5cm
Notes: That is why we will be testing Inconel 625 in various direction to fully understand how the material behaves under the influence of its new texture. From the new dynamic forming process, we will also have to understand how the material behaves at low and high strain rates. To test these conditions, we are using a servo hydraulic test machine so we can achieve the low strain rates of 10 to the -4 and 10 to the -1/s. To achieve the strain rates closer to 1000/s, we will be using a Kolsky bar.
MTS is actually the trade name of the machine. I know MTS is probably in all your plots, so lets keep it, but ordinarily we would just say “servo-hydraulic” load frame. Also, FYI, the load frame applies force by the use of high pressure fluid (hence it is called a hydraulic load frame). There are other kinds of testers that use a screw (screw-driven machines) and others that use an electromagnetic coil (for low loads), FYI

## Slide 8
NIST IN625 Tension Specimen vs ASTM E8 Standard
NIST Tension Specimen
ASTM Standard Tension Specimen
1. Specimen uses the full thickness of sheet for a .5 mm thickness
1. Requires the specimen to use the entire thickness of the sheet metal
2. The gage length is designed to 7 mm because of the limitations of the applied force and displacement of the Kolsky Bar
3. The Gage length to gage width ratio is 4:3
4. Ensures a strain of ~.35 for each test, assisting with the likelihood of capturing fracture
2. Requires a minimum gage length (G) of 32 mm for each specimen
3. Gage length to gage width ratio of at least 4:1
4. If all suggestions are applied to the NIST Tension Specimen for the Kolsky Bar, a strain of .11 would be achieved.
Notes: The kolsky bar is a great tool to understand how large strain rates affect the mechanical behavior of a material, but it also has its limitations that need to be accounted for. There is a standard test method for testing metals in tension, and in that standard it specifies how the test specimen must be designed. Although we follow a few guidelines, like using the entire thickness of our .5mm sheet of Inconel 625, we fall once we get to the recommended gage length. The ASTM E8 standard requires a 32mm gage length, while we were forces to design it to only 7mm. This is because the Kolsky bar can only stretch the sample a certain length during the time of the test, and we need to achieve a strain that would get us close to fracture. From that, we do not follow the guidelines of E8, but it does allow the test to occur so we can discover useful data on its behavior at these high strains.
E8 is not only specimen but also testing rates, (usually slow)

## Slide 9
Testing Conditions – High Strain Rate
A Split Hopkinson (Kolsky) Bar is utilized to achieve a strain rate of at least .
This strain rate is crucial to understand for its applications in aerospace and high speed machining. These areas exhibit the types of conditions seen from a Kolsky Bar test.
Notes: Pictured to the right is the Kolsky bar, designed for strain rate around 1000/s, which is crucial to understand for the applications that see these strain rates, like dynamic forming, high speed machining, and automobile crashes.

## Slide 10
Kolsky Bar: Basic Mechanics
But, the deformation velocity is only about half the striker velocity
(~ 8 m/s here)
2 mm thick sample
at 30,000 frames per second
Pulses Travel at the Speed of Sound in Steel (~ 5000 m/s)
Test Sample
Stress-Strain
Strain Rate
Notes: The Kolsky bar functions by introducing a striker bar that hits the incident bar, pushing a compression wave towards the sample, and producing a reflected and transmitted pulse. These pulses are then collected by the strain gages on each bar which is then able to graph a stress strain curve of the experiment at the strain rate experienced. These pulses move at the speed of sound in steel, roughly 5000m/s. Although this example was for compression, which we will see in a few minutes, tension is can also be accomplished by inverting the striker bar impact direction.
Whole tests lasts about 0.1 milliseconds
Simple compression. Also have the ability to work in tension.
Tension as well, pulls instead of pushes on

## Slide 11: 3D Digital Image Correlation (DIC)
20 pixels
20 pixels
3D Displacement
3D Initial Position
Image Pair “Subset”
Overlapping Image “Subsets”
Cameras
Sample
(Image from one of the cameras)
Allows us to measure SHAPE, DISPLACEMENT and STRAIN locally on our tension samples
Notes: Another, more modern, way of collecting our data during the tension tests is using 3d Digital image correlation. This setup requires two high speed cameras looking at the specimen during the test. The specimen is painted at the gage section with a white background and black speckles. The cameras are then able to track these speckles as the gage deforms, producing the shape displacement and strain locally for each frame captured during the test.
Measures strain not stress duh

## Slide 12
Kolsky Bar Tension Test
Notes: Here is a movie from one of our tensile tests, showing the movement of the specimen as the tensile waves passes through. You can also clearly see the speckled paint on the specimen, so the cameras can produce a graph detailing its deformation through time.
When paint delaminates, DIC is useless and stops
Bad correlation

## Slide 13
High Strain Rate Test Results
Notes: This graph details the results from the high strain tests at the various orientations. There is definitely some scatter, including an error in one of our rolling direction experiments, but you can begin to see a trend in how the material behaves.

## Slide 14
High Strain Rate Test Results - Average
Notes: If I bring up the average values of each direction, you see that the rolling direction, the orientation that moves with the microstructure, shows less strength throughout the stress strain curve. But also note the error bar, which is a calculation of error propagation estimated from the test that could lead to the orientation not being significant in mechanical strength.

## Slide 15
Low Strain Rates
A Split Hopkinson (Kolsky) Bar is utilized to achieve a strain rate of and .
This strain rate is important to understand for its mechanical properties when it is subject to a increasing load over a longer period of time.
Notes: Pictured to the right is the servo hydraulic testing machine that was used for our slower strain rates. It is also important to understand how Inconel 625 behaves under an increasing load over a longer period of time . Because the lamina being deformed via the dynamic forming operation is experiencing many strain rates simultaneously (including the maximum one) we need to understand how this material behaves over a wide range of strain rates

## Slide 16
MTS Test Results - Slow
Notes: These data here were gathered over a time interval of around 2 hours due to such a low strain rate of 8.7 * 10^-4/s. With these curves, it shows that each orientation behaves almost identically with each other, meaning the texture and orientation at these low strain rates do not play a crucial role in its mechanical behavior in tension, but rolling direction is slightly favored.

## Slide 17
MTS Test Results – Slow - Average
Notes: You can see this more clearly when the averages are displayed for each specific orientation. The error bars also show that the error propagation is significant enough to not conclude that rolling direction behaves far differently then the other directions.

## Slide 18
MTS Tension Test
Notes: Here is a video of what the DIC records during the test. As the test progress’, the strain near fracture increases until fracture occurs. The speckles painting on the specimen allows these cameras to make the measurements.

## Slide 19
E8 vs. High Rate Specimen
Notes: One point that is extremely important to verify is if our tension specimen yields vastly different results due to its different design compared to the E8 standard specimen. This graph illustrates this exactly. The red lines is the data collected at the University of new Hampshire using an ASTM E8 specimen on an MTS, where the green shows our tension specimen data on the MTS. Although there is a slight disagreement at the later strains, these data are very similar, especially taking into account the error bar shown.
Forced to use non standard specimen, and we wanted to see that this choice caused any significant problems to measuring the mechanical behavior in tension from the standard E8
Did you assume .5mm for every sample or did you measure each one?

## Slide 20
E8 vs. High Rate Specimen
Notes: We see these same results in each orientation, like here in the transverse direction.

## Slide 21
Strain Rate Sensitivity
Notes: By testing multiple strain rates, we are able to see how strain rate effects a certain orientations mechanical behavior clearly. Apart from the high strain rate outlier here, you can begin to see trends…
Positive, higher strain rate, higher YS and yield

## Slide 22
Strain Rate Sensitivity
Notes: These averages clearly show how each strain rate can affect the mechanical behavior of the material including how much strain it can take before fracture.

## Slide 23
IN 625 Compression Specimens
The IN 625 compression tests will be used to probe its deformation mechanics
These data will derive the parameter of thermal softening in the Johnson-Cook equation,
Allows us to better design the lamina part
These specimens are manufactured using an EDM taken from the material of an Inconel 625 plate.
The characteristics were very similar to the Inconel 625 sheet used for tension
4mm
Notes: Another important effect the material will undergo during dynamic forming is temperature change. We chose to use compression specimens for our heating data because it is far easier to heat compression specimens then tension specimens, and the graph on the bottom right shows that choosing the compression specimens for temperature testing did not significantly affect its stress strain curve, allowing us to trust the data we get from the tests.
Compression tests at high rate and T because we want to find the thermal softening rate of IN 625. Dynamic forming has high speeds and short times, adiabatic heating, heats up from plastic work, and its important to know how the strength of IN 625 varies with Temp
Doing this in compression because it is simpler experimentally to get the results
Graphics bigger
Not the .5mm sheet, used thicker plate. Differences in rolling? Nope, looks very similar

## Slide 24
Pulse-Heated Compression Kolsky Bar
Samples are heated electrically in a few seconds prior to high strain rate compression test
Mates, SP; et al., EXPERIMENTAL MECHANICS, 48 [6], 799-807, 2008
30,000 fps movie, heating to 800 °C in 1 sec with 2 second hold prior to impact
Notes: As a kolsky bar outfitted with pulse heating, the mechanics is nearly the same, except prior to mechanical impact, a battery banks supplies a large amperage to the specimen, allowing it to be heated to nearly 1000 C in just a couple of seconds. The current is then cutoff and is immediately followed with mechanical deformation.

## Slide 25
Compression Test Results – All Temperatures
Notes: This busy graph show how the mechanical strength drops as temperature increases, a well-known trend in materials science. All the data we gathered, including strain rate and temperature effects, will allow us to calibrate a model for Inconel 625 that is suitable to simulate the dynamic forming process shown earlier.

## Slide 26
Constitutive Model
Johnson-Cook plasticity
  Accounts for temperature, strain rate and plastic hardening
  Simplest model (fewest coefficients - 5) that captures these combined effects
  Combines with Linear Elasticity in Finite Element Model
Johnson-Cook Model
Notes: The Johnson-Cook model is a well-known equation that captures strain rate and temperature sensitivity of mechanical strength, and it works well for many metals. The parameter values needed for Johnson-Cook model, which will allow us to correctly design the dynamic forming process, are thermal softening, rate sensitivity and yield and hardening parameters.

## Slide 27
Johnson-Cook Slide – NOT DONE

## Slide 28
Conclusions
Measured the mechanical behavior of Inconel 625 sheet metal at various strain rates and orientations to determine the rate sensitivity and strain hardening behavior.
Measured the compression behavior of Inconel 625 plates at high strain rates with rapid heating before deformation to determine the thermal softening.
Obtained reliable data to understand to fit Johnson-Cook model to simulate the dynamic forming of the lamina component in a heat exchanger.
Notes: Overall, during this Summer we were able to measure the mechanical behavior of Inconel 625 at various strain rates and orientation to its rolling texture and test the thermal softening of the material in compression. These data will then be able to be fit to the Johnson-Cook flow stress model that can then accurately simulate the dynamic forming of the lamina component ins a heat exchanger. Thank you.
Scatter plot, repeat measurement, shows scatter with stress strain, tough to handle thickness of very small specimens. Plot new one with average value, less scatter

## Slide 29
Questions?

## Slide 30
B. Paul. “Low-Cost Waste Heat Recovery Using ‘Half-Array’ Microchannel Heat Exchangers”. Oregon State University, lecture
References

## Slide 31
Compression Test Results – Room Temperature

## Slide 32
UNH Verification Slow Strain Rates