## Slide 1: Development of a new specimen configuration which allows for the investigation of stress triaxiality effect on flow and fracture behavior of ductile materials.
A Shear Compression Disk Specimen with Controlled Stress Triaxiality under Quasi-Static Loading

## Slide 2: The Experimental Setup
Confining Holder and Spacing Ring
  Used to achieve the required pre-stress on the specimen by matching the inner surface of the confining holder incline angle to the specimen.
  Spacing ring used to set the insertion distance of the specimen.
Specimen
  Forced into the confining holder and spacing ring that generates pre-stress. Magnitude depending on the angle chosen for the confining holder and specimen.

## Slide 3: Experimental Procedure
Contain specimen in confining holder so that the pre-stresses on the specimen are present with an insertion of height H.
Apply a ‘main load’ to the inner disk of the specimen.

## Slide 4: Experimental Results
Used 4340 steel with specific characteristics
Differed only in tilt angle, beta.
The smaller tilt angle results in lower triaxiality of the specimen
Recorded the true stress and strain of the material during the test
Simplifies the test, stress triaxiality can be controlled only by the choice of geometrical parameters.

## Slide 5: A Shear Compression Disk Specimen with Controlled Stress Triaxiality Under Dynamic Loading
The Shear Compression Disc (SCD), is examined for its adequacy for the investigation of the effect of triaxiality and strain rate on plastic flow and fracture.

## Slide 6: The Experiment Setup
Specimen identical to quasi-static experiment
An adapter is used to help hold the specimen between the transmitting and incident bars
The experimental procedure is identical with the angles of the parts defining the pre-stress the specimen experiences.

## Slide 7: The Experiment
12 tests conducted, 7 without a preload and 5 with a preload on the specimen.
Different specimen angles chosen to cover a wide range triaxiality levels.

## Slide 8: Discussions
Are the results repeatable every time within reasonable limits?
  Yes
If the SCD specimen is capable of characterizing a correct fracture strain, at any given triaxiality level and strain rate, within a reasonable limits.
  Additional results needed